## Slide 2
(a) Layered crystalline structure of the rhombohedral LiCoO2; (b) representation of the octahedral CoO6structure; (c) stacking arrangement of the layers (ABCABC)
(Ref: Synthesis and Characterization of LiCoO2from Different Precursors by Sol-Gel Method)
each O is shared by 3 CoO6  CoO2

## Slide 3
Ref: Coo2, the end member of the LixCoo2 solid solution
CdCl2
CdI2
http://www.chemtube3d.com/solidstate

## Slide 5
With this result, it is not possible to determine the position of phase boundaries without ambiguity. In fact, the electrochemical behavior below x=1 / 3 is controversial among previous literatures

## Slide 6
Ref: First-principles investigation of phase stability in LixCoO2
Electronic phase diagram of the layered cobalt oxide systemLixCoO2(0.0≤x≤1.0)

## Slide 7
Ref: Electrochemical behavior and Li Diffusion study of LiCoO2 thin film electrodes prepared by PLD
Ref: First-principles investigation of phase stability in LixCoO2

## Slide 10
J. Electrochem. Soc., Vol. 139, No. 8, August 1992

## Slide 15
2nm SEI formed on the surface of LiCoO2 after soaking in DEC for 1 hr at 25°C
1nm SEI formed on the surface of LiCoO2 after soaking in LiPF6-electrolyte (EC:DMC=1::1) for 1 hr at 25°C
XPS data of Co composites

## Slide 16
SEM characterization of P-LCO and D-LCO particles after the cycling test. a, The SEM images of P-LCO. The inset shows an image with high resolution. b, The SEM images of D-LCO.

## Slide 18
Pristine LiCoO2
Al2O3 coated LiCoO2

## Slide 19
Pristine LiCoO2
ZrO2 coated LiCoO2